## Slide 1: Normal Metal Interaction
So our H is:
q sum in Veph is over all wavevectors, even those outside the BZ. But note that Ωq and Aq are periodic functions of q over volume of BZ.

## Slide 2: Normal Metal Interaction
Now we’ll consider the effective interactions, whereby we may roughly encompass the effects of one interaction within the other.
Electron-Phonon Interaction
Ignoring vertex corrections to the interaction (which are supposed to be quite small according to Migdal’s theorem), we can incorporate the e-e interaction into the e-ph interaction by summing all diagrams whereby an electron scatters into another state and gives off a phonon. We’ll recognize the exact density-density correlation function there.
And it simplifies to:
Getting a little ahead of ourselves, since g always comes in combination g2D, we can make cosmetic change,
and so new g is same as old g, but with renormalized frequencies, Ω -> ω, and a screened electric potential.

## Slide 3: Normal Metal Interaction
Now we’ll consider the effective interactions, whereby we may roughly encompass the effects of one interaction within the other.
Electron-Electron Interaction
We can write the effective e-e interaction as the sum of two terms. Sum of all scattering via which is initiated by e-e field, and those that are initiated by e-ph interaction.
And it simplifies, in the RPA approximation (allows ignoring vertex corrections), to:
Exact(ish) phonon GF.
(irreducible density-density correlation function). Λ is defined by equality:

## Slide 4: Electrons - Excitations
Electron Self-Energy
The electron-phonon interaction doesn’t change the energy of the electron much except near the Fermi surface, where it often dramatically alters the effective mass. Metals which experience high mass renormalization are often good superconductors.
We’ll estimate the self-energy using the ‘first’ order diagram, but with the full phonon GF, and vertex, out to RPA.
The entire correction looks something like this:
This turns out to be mainly negligible except close to the Fermi surface, where we get a large mass correction.

## Slide 5: Phonons - Excitations
And eventually we find, using our RPA result for Π, that we can approximate the pole as being at, in small q limit:
Phonon Self-Energy
The phonon energies do change, like before, because the electrons do drastically screen the ions motions. Let the ‘self’ energy be the polarization bubble (not just the irreducible part). Then,
So we get:
And so the excitations are now ‘acoustic’, i.e., linear for small q.

## Slide 6
Phonons – Excitations
To make practical calculations we approximate the excitation spectrum like this:
where we approximate the 1st BZ as a sphere with radius kD ( ~ kF) such that same number, N (= number of lattice sites), states are encompassed. We would expect this sphere to extend past the 1st BZ at points.
And the acoustic spectrum is presumed linear with k (as the real one is, for small k), so that we just get cones of different slopes. The optical spectra are presumed entirely flat. Since vs ~ 100m/s, the topmost acoustic energy ED << EF. And so at room temperatures, we can expect all the acoustic spectra to be partially occupied with excitations. But the optical spectra are quite high and so we wouldn’t expect thermal occupation.

## Slide 7
Specific Heat
We can calculate the phonon part of the partition function; we’ll use the renormalized acoustic phonon dispersion relation, i.e., the Debye model.
Working this out gives us (for acoustic spectrum (ω = ck) we get the T3 law (TD ~ 100K) for low T’s. And it asymptotes to the classical value at high T. Optical modes are unlikely to be thermally populated before melting point. But if they were, then the heat capacity would go up in step-like fashion as each additional optical mode begins to be occupied.
Phonons – Thermal Equilibrium Properties

## Slide 8: Transport Properties
Conductivity
Now let’s consider the semi-classical approach to calculating the conductivity.
We will implicitly be using the RPA twice renormalized e-ph interaction, The collision integral will look something like this:
Taking the functional derivative of this, we can get 1/τ (see relaxation time approximation to Boltzman equation). Then sticking that 1 – cos(p,p’) factor in there, thermal averaging over all Nq, etc., we end up with 1/τtr, and then plugging that into σ, we have:
note the T5 drop in resistivity is dependent upon the linear acoustic phonon spectrum. So if ‘acoustic’ modes were unscreened, I’d think we’d get a larger contribution.

## Slide 9: Transport Properties
Conductivity
Now let’s consider the effects of impurities….a good approximation at high T is Mathieson’s rule, which posits:
We can take account of large weak localization by simply replacing the zero-phonon phase breaking length L, with Lph ~ √(Dτph). In the strong localization case, when all nearby states are localized, I believe the resistivity temperature dependence is something like exp(1/T1/4) (Mott hopping?). Here transport occurs by phonons exciting electrons from one localized state to another. A qualitative argument for this law is as follows. Probability of hoping to another state is product of P(jumping to that energy)×P(jumping to that position). Both of these probabilities are approximately exponential, when states are localized.
Assuming states are isotropically distributed, we have:
Filling this into P, and choosing the R which maximizes P, and asserting that P ~ σ, we have:
So we’ll note that as decrease T, conductivity will increase, and level off to a constant, unless disorder is high enough that system is in insulated state, in which case the conductivity will actually drop to zero as LT (phase breaking length) surpasses the sample length.

## Slide 10: Nonequilibrium Properties
Now we’ll consider the dielectric susceptibility. So from the definitions of all the susceptibility functions (see EM folder/Metal ME perhaps) we can say that the total ε follows the equation below,
and we can relate the total ε to the electron εe and the phonon/ion susceptibility εion.
recalling the bare susceptibilities (treating electrons and phonons as separate here, so can’t include screening in the phonon dielectric), in the roughest approximation,
combining these, we find:
and this congrues with what we found when looking at the effective interaction a few slides back.

## Slide 11: Phonons – Nonequilibrium Properties
Absorption
Photon absorption by phonons works pretty much like it does with electrons. Can’t really have absorption within the same band, but can between different bands. If between different acoustic branches, then it’s called Brillouin scattering, and if between acoustic and optical branch, then Raman scattering. I think the latter predominates; it seems its more likely for an optical branch to be excited by, well, optical photons, because oscillations of this branch involve out of phase oscillations of atoms in the basis which are often oppositely charged, and so kind of resembles wave antenna current oscillations, or oscillations of electrons when making transitions between atomic states, and so more easily receives and creates EM radiation.

## Slide 12: Phonons – Nonequilibrium Properties
In a periodic potential, only crystal momentum is conserved (and that, only up to RLV). With the extra G in there, we can connect two points on the dispersion curve with a photon line (the red one, ultimately). So we can get absorption in periodic potentials.
In the reduced zone scheme, it’d look like this:
starting point
And in the reduced zone scheme, it’d practically look like this, because the slope of the photon line is so steep compared to the electron dispersion curve. So basically we need only worry about energy conservation, graphically.

## Slide 13: Superconductors - Interaction
At very low temperatures, many metals will enter a superconducting state. The metal must have a strong enough e-ph interaction to induce a sufficient attractive force between e’s. And the metal must have a large enough electron density of states. Or well, the critical temperature below which these metals would superconduct depends on these parameters. Basically Tc ~ exp(-1/λρF). So if the electron-phonon coupling is weak, then λ will be small. And if density of states is small, then ρF is small obviously. And this would make Tc super small, perhaps beyond presently achievable temperatures. Additionally, the metal has to support its electrons joining up in ST = 0, i.e., ↑↓ singlet pairs. So Alkali/Alkaline metals don’t superconduct (at achievable temperatures anyway) because their density of states is too small and or their electron- phonon coupling is too weak. But the transition metals often do superconduct, as often their Fermi surfaces intersect the d-bands and so their density of states is large; the Noble metals are an exception. But the transition metals that have a ferromagnetic phase transition at low T’s will not superconduct, because their spins would tend to want to pair the wrong way, i.e., ↑↑ or ↓↓. Aℓ does have a barely strong enough coupling strength and density of states to superconduct. Some metals, like Pb, couple very strongly, and require the Eliashberg theory for an adequate description.

## Slide 14: Superconductors - Interaction
BCS Theory
So if we go back to that effective e-e interaction,
Can see we get attractive interaction for energy transfers ω < ωq. For electrons near Fermi surface, momentum transfers q, will be such that q ~ qF and so ωq ~ ωD. So now near the Fermi surface, we have a negative interaction for ω < ωD, roughly. If energy transfers are with ωD of Fermi surface, then energies themselves are within that range too. So we can represent the effective two-particle interaction as roughly,
The small attractive potential is mainly effective at binding electrons near the Fermi surface, specifically, within about a Debye energy of it. Electrons enter the bound state in pairs (k,↑) + (-k,↓). And so one often restricts the interaction to include just these guys, and so we say (1/2 goes away due to spin sum):
This is the one most often used, actually

## Slide 15: Superconductors - Interaction
BCS Theory
Mahan does it differently. He replaces ω w/ ξq (I guess), and gets:
So we get attractive interaction when ξq < ωq, which means εq is close to Fermi surface. And if q is close to Fermi surface, then ωq ~ ωD. So can say,
And so we might say, roughly,
Another potential approximation is to just extend the k-space range of (constant) attraction to everywhere, and then we get this, basically a delta function interaction in position space. ,

## Slide 16: Superconductors - Excitations
There are a few ways to investigate the excitations. We’ll take the approach where we look at eigenstates of the two-body interaction. The relative Schrodinger equation is given below, and we’ll take the interaction to be the guy on the right. K is the momentum of the center of mass. M and μ are the total mass, and relative mass, respectively.
And we want to ascertain what the lowest energy state of the system is. We suppose our two particles initially reside on the Fermis surface, with equal/opposite momenta (b/c we’re looking for lowest energy state). So then EKn = 0 + εn. And we want to see if we can get a solution whereby EKn = εn < εF + εF. (i.e., that the potential energy does lower the energy of the pair below the sum of their respective kinetic energies). This isn’t forgone because for attractive spherical well potentials, the energy spectrum is the same as the free particle spectrum, at least if the potential isn’t strong enough. To make progress, since our potential is given in terms of the wavevectors, we take the Fourier transform of both sides,
So under our approximation, the potential is separable, and doing some algebra, integrating both sides w/r to d3q, etc., we end up with an equation for the energy:
So we get the approximate solution above, which is indeed lower than the kinetic energy sum. Might note that this is non-analytic function of λ.

## Slide 17: Superconductors - Excitations
We can improve our analysis by looking at the many-body problem, and looking for the many-body ground state.
Apparently it’s a pain to fashion an explicitly N-particle state. So we will fashion a state with an unspecified number of particles. k’s range over all values allowed by boundary conditions (BZ).
Minimizing w/r to φk, we find.
Normalization
Particle Number
Then we want to minimize H subject to constant particle expectation. So we form K = H - μN. The μ here is the same μ that appears in Vs. Seems to beg for some justification, but whatever.
The stronger the interaction is (λ), the larger the gap (Δ) is. Physically, we have depletion of particles below the Fermi surface and repletion (?) of particles above it. This increases kinetic energy, as apparent, but overall decreases energy because (some of) these guys in that region are forming a Cooper pair and lowering the overall energy via the potential interaction.
Energy of GS (to order Δ2), where εF0 is free Fermi energy.

## Slide 18: Superconductors - Excitations
Now we’re going to use a MFT approach to examine the excitations of the BCS Hamiltonian. So we start, again, with:
Not sure exactly why - probably has to do with fact that it kind of acts as order parameter - but we’ll take our mean field term to be the guy in the GS wavefunction. Brackets we’ll take to mean thermal average (in Grand Canonical Ensemble):
With this we want to form K = H - μN. Our H (and K) is bilinear in the creation/annihilation operators, and so we need only find the linear combination that will diagonalize it. This is given by Bogoliubov-Valentin transformation:
So we write this pair of operators, as the sum of its mean field value + fluctuations about:
In terms of this, we can write the Hamiltonian, to first order in fluctuations, as, introducing definition (in present context) Δk:
And we get:
Can sort of treat the ξ as single particle spectrum in the |k-kF|> kF limit. And we’d have,
So a T-dependent gap opens up in spectrum, which goes to zero as T -> Tc.

## Slide 19: Superconductors - Excitations
Now we’re going to analyze some GF’s
We’ll first do the singlet-singlet GF:
And looks like we’ll use the ladder approximation.
This works out to:
We’re interested in the long wavelength, static limit; so we take q  0, and ω (iν)  0. And we find:
Plugging this into R, we find a singularity will be present at the following temperature:
The instability indicates something fishy is happening at this temperature. But what could it be!?

## Slide 20: Superconductors - Excitations
Now we’re gonna switch to this (the usual) Hamiltonian:
And calculate the standard single particle GF:
Instead of using the customary diagrammatic expansion, we’re going to apply MFT to the PDE satisfied by the GF (now calling GC*σσ’ simply G):
Now we’ll use MFT by applying Wick’s theorem to the fully interacting c’s in the bracket. But now we’re going back to the conceit that we’re dealing with many-body states of indeterminate number so that we can have non-zero expectations of any pair of c’s. This necessitates expanding our GF’s of concern to the following set of three, to the right. And then proceeding with Wick’s theorem, we find the following self-consistent set of equations.
Taking Fourier transform, we can solve, to find:
And then can plug F into the Δ equation, and solve for Δ self-consistently, to get what we’ve found before:
And we can clearly see the excitation spectrum from the GF’s denominator, as we found before.

## Slide 21: Superconductors - Excitations
Now say we add impurities to the mix,
We can develop a perturbative expansion of the 3 (four really) GF’s introduced in previous slide. First we put them together in the Nambu formalism,
Diagrammatically, these are associated as follows with the correlation functions below:
The unperturbed GF’s are the same guys, but w/o the bars on them. Note I’m not putting 0’s on them because we are including the MF interaction in our ‘unperturbed’ GF’s, so they’re not ‘free’ GF’s. We’ll want the Fourier transforms, and this is (σ’s are Pauli spin matrices):
And then we connect the external points on left, with the disorder vertices on right. We have two of them because we can now connect to either end of the vertex since we’re averaging over indefinite particle number states. Of course the disorder average enforces momentum conservation from the vertices, etc, see the Electron/Impurity file for more on that.

## Slide 22: Superconductors - Excitations
Okay, we can work out a self-energy equation. This is the one for C*. The <<, <>, ><, >>, mean that the self energy diagrams begin and end with that part of the vertex.
If you check out the QM/Identical Particles/Self-Energy file, we can reason by analogy that we can write out a matrix self-energy equation.
Assuming a spatially homogeneous substance, this would come out to,
We could do a first order Born approximation on the self-energy (see Electrons/Impurities/Excitations for comparison)
Diagram translates to this guy, and in second line we presume delta function interaction.

## Slide 23: Superconductors – Thermal Properties
Guess we’ll start with the heat capacity first, at least within the mean field approximation. So back in that file, we found:
And so we can form the Grand Partition function.
And from this, we can get the Landau free energy:
From this we can form entropy (see arguments in Stat Mech file for independent fermions, as they apply here too).
And then can get heat capacity:
From this, we find:
And we get that graph above. There is no singularity at Tc, just a discontinuity, given by:

## Slide 24: Superconductors – Thermal Properties
Now let’s examine the Meisner effect (namely that magnetic flux is completely expelled from Type I superconductor as B changed).
For type I SC’s, at any T < Tc, as increase field eventually it becomes energetically (and thermodynamically with entropy and all I’d guess) for the Cooper pairs to break out of their anti-aligned S = 0 state and align with the external field. This will apparently happen en masse at a certain critical field Hc, so that except near Tc, the transition is first order. Since the GL Free energy describes 2nd order phase transitions, it would not be able to describe this process except near Tc.
For type II SC’s, at any T < Tc, as increase field, eventually, at Hc1 it seems the Cooper pairs lose mobility and are confined to an increasingly small region of the SC? The radius of this region goes from ∞ at H = Hc1 to 0 at Hc2. Accordingly, magnetic flux begins to permeate the SC at H = Hc1 through what are called vortices, whose radii increase from 0 to ∞ as H progresses to Hc2. So SC is destroyed by the time we get to H = Hc2, and this transition is second order.

## Slide 25: Superconductors – Thermal Properties
First we’ll do the London theory. We assume there is a certain density of superconducting electrons ns. Then, according to N2L, and Maxwell we have those three equations. In the latter though, we’ll take out the dE/dt term as this describes EM wave propagation and we’re going to presume we’re doing this in a quasi-equilibrium manner, so no waves. Also, we’ll confine our attention to inside of metal so we can take jf = 0.
Can combine first two to get:
And if choose integration constant to be 0, then we have:
Then plug that into other ME and we get PDE for B. Can solve and see that B field exponentially decays to 0. Length scale of decay is the penetration depth,
The lines are total B field lines,
where φ would be just ‘some’ function.
Note that we presumed ns constant in space here. Otherwise our B field PDE picks up a source term, and it doesn’t follow that B must exponentially decay – this is where Type II’s differ from Type I’s, and how they let B flux in.

## Slide 26: Superconductors – Thermal Properties
Still on Meisner Effect. But now we’ll do it with QM, and in the process get a formula for ns(T). Our H is:
If take a look at the Conduction file, can see that this will reduce to:
Since we want to see how j responds to the magnetic field when we slowly and uniformly turn it on (‘cause that’s what we were implicitly doing before – ‘cause recall we had to do it slowly enough to neglect the dE/dt term in ME) we will set q = ω = 0 in K. When we do this, filling in the G we got from the excitation file, we find,
We can identify all that as ns by comparing with the form of our result with the London theory (also presuming φ = 0 FWIW).
And from Electrons/Impurities/Conductivity or something, we should recall the relationship between current and vector potential.
This is our diagram. The G’s are full e-e interacting G’s -

## Slide 27: Superconductors – Thermal Properties
Still on Meisner Effect. But now we’ll throw in impurities. So now we have for H:
If take a look at the Conduction file, can see that this will reduce to:
Since we want to see how j responds to the magnetic field when we slowly and uniformly turn it on (‘cause that’s what we were implicitly doing before – ‘cause recall we had to do it slowly enough to neglect the dE/dt term in ME) we will set q = ω = 0 in K. When we do this, filling in our G, I think we find the same thing,
We can identify all that as ns by comparing with the form of our result with the London theory.
And from Electrons/Impurities/Conductivity or something, we should recall the relationship between current and vector potential.
We approximate the disorder average diagrams with just the first (no impurity ladder). The G’s are full e-e interacting G’s and disorder averaged (w/in Born approximation, say)

## Slide 28: Superconductors – Thermal Properties
Now we’re going to reprise our analysis by first ‘deriving’ the (Ginzburg-Landau) Free Energy of a superconductor in an electromagnetic field. We’ll start with the following Hamiltonian,
with this we can construct the (grand) partition function,
then we’ll use a Hubbard-Stratonovich identity
to decouple the interaction term, and write:

## Slide 29: Superconductors – Thermal Properties
We’ll make it cleaner by introducing the Nambu spinors, and GF,
then expand the GF-1 out,
We can factor out the free partition function, and say,

## Slide 30: Superconductors – Thermal Properties
Now we’ll write down the Feynman rules for calculating the diagrams involved in this expectation – note we’ll want to go out to 2nd order in A and fourth order in Δ.

## Slide 31: Superconductors – Thermal Properties
Terms of order Δodd are zero, because Trace gives us zero. Some of the non-zero guys are:
Assuming A and Δ are time (τ)-independent, this reduces to:
expand to lowest order in q’s, as we’re looking for low energy excitations.
so we come to this,

## Slide 32: Superconductors – Thermal Properties
Terms of order Δodd are zero, because Trace gives us zero. Some of the non-zero guys are:
Assuming A and Δ are time (τ)-independent, this reduces to:
expand to lowest order in q’s, as we’re looking for low energy excitations.
so we come to this,

## Slide 33: Superconductors – Thermal Properties
Terms of order Δodd are zero, because Trace gives us zero. Some of the non-zero guys are:
Assuming A and Δ are time (τ)-independent, this reduces to:
expand to lowest order in q’s, as we’re looking for low energy excitations.
so we come to this,

## Slide 34: Superconductors – Thermal Properties
Terms of order Δodd are zero, because Trace gives us zero. Some of the non-zero guys are:
Assuming A and Δ are time (τ)-independent, this reduces to:
expand to lowest order in q’s, as we’re looking for low energy excitations.
so we come to this,

## Slide 35: Superconductors – Thermal Properties
Filling these back into our partition function, and putting things into the exponent, we have:
So we can identify the free energy functional as:
Filling in our results, rescaling the field, we come to the following (note we moved the * from ρF to m):

## Slide 36: Superconductors – Thermal Properties
So that’s our free energy functional. But actually, we will want to add in the magnetic field energy, since A is the total vector potential. And our F will be the free energy of the superconductor plus field. IBP will put it in the following form,
The s on F means that this is just the superconducting part of F, i.e., F(λ) = [F(λ = 0)] + [F(λ) – F(λ = 0)] = Fn + Fs, where λ is the interaction strength from all the previous slides.
Worth noting two intrinsic length scales. The correlation length is pertinent to Type II’s predominantly. It gives the radius of the flux vortices that penetrate the metal. Also, higher it is, the ‘stiffer’ the superconducting electron lattice, and the higher the energy cost to inducing spatial fluctuations in ns. Already discussed λ.
e* and m* are the effective charge and mass of the entity that the ‘wavefunction’ describes.

## Slide 37: Superconductors – Thermal Properties
Now to get the actual free energy, not just the functional, we need to minimize it w/r to the free internal parameter, which is the pair density amplitude ψ. So we take functional derivative and get the following equation.
So then we can say the actual Free energy is given by:
Usual derivatives give us the free current and the superconducting entropy,
Working this equation out we get the bound current, i.e., the superconducting current.

## Slide 38: Superconductors – Thermal Properties
Type I. So let’s see what it says about Type I’s. Apropos the Meisner effect, recall we found,
Working this out a little, we have:
So we get the London equation if we can assert that the phase φ is constant. And we get the Meisner effect if we can say that ns is constant. If we can use our result for ψeq when fields are absent, namely ψeq = [-r/u]1/2, then ns* would go as –r/u, which implies linear T dependence near critical point.

## Slide 39: Superconductors – Thermal Properties
Now let’s consider the critical Hc(T) curve for Type I’s. We want to determine where, for fixed external field Bf = 4πH (assuming solenoidal geometry and all), the superconductor will prefer to be in a superconducting state vs. normal metal state. Since we’re holding T and H constant, not T and B, we need to perform a Legendre transformation to the correct free energy F*.
See when it is thermodynamically more favorable to be in normal metal state (ψ = 0, H permeates) vs. SC state (ψ = ψeq = (-r/u)1/2 and H eliminated)
And we find:

## Slide 40: Superconductors – Thermal Properties
Type II. So let’s see what it says about Type I’s. Apropos the Meisner effect, recall we found,
Working this out a little, we have:
So we get the London equation if we can assert that the phase φ is constant. But the deal with Type II’s is that ns isn’t spatially constant, and so that is why flux is not (completely) expelled.

## Slide 41: Superconductors – Thermal Properties
Now let’s consider the critical Hc2(T) curve for Type II’s. We want to determine where, for fixed external field Bf = 4πH (assuming solenoidal geometry and all), the superconductor will prefer to be in a superconducting state vs. normal metal state. Since we’re holding T and H constant, not T and B, we need to perform a Legendre transformation to the correct free energy F*.
See when it is thermodynamically more favorable to be in normal metal state (ψ = 0, H permeates) vs. SC state (ψ = ψeq(x) and H small but constant)
Remember we can get B in terms of H via:
We presume small constant A, neglect the u/4 term. Then ψeq equation becomes simple Schrodinger equation in magnetic field. Then use variation of parameters to find combination that minimizes F, and thence F*.
Whether a superconductor prefers to be Type I vs Type II depends on whether it hits Hc(T) vs Hc2(T) first as descend from high H values.
So if ξ is small, then energy cost of inducing spatial fluctuations is small, and superconductor tends to be Type II.

## Slide 42: Superconductors – Nonequilibrium Properties
Now want to look at the absorptivity and conductivity. Our H is:
We’ll recall our conductivity tensor is:
So we connect the endpoints together via the interaction vertices shown. But note that we can connect to either end of vertex and endpoints since particle number is indeterminate.
And then we can write this in terms of the Nambu matrix GF…
All the vertex insertions just serve to give us the full (equilibrium) GF’s. The direct connections are G’s, and the cross connections are F’s.

## Slide 43
Now want to look at the absorptivity and conductivity. Our H is:
Our conductivity tensor was given in previous slide, and if we want the absorbtivity then we take the real part, and then can take the q = ω = 0 limit to get the DC conductivity too.
So we simply have to evaluate this guy, where the G’s are fully interacting ones.
And we get:
T = 0, ω ≠ 0.
T ≠ 0, ω = 0.
Superconductors – Nonequilibrium Properties

## Slide 44: Superconductors – Nonequilibrium Properties
Now want to look at the (disorder averaged) absorptivity and conductivity in the presence of impurities. Our H is:
Our conductivity tensor was given in previous slide, and if we want the absorbtivity then we take the real part, and then can take the q = ω = 0 limit to get the DC conductivity too.
The simplest approximation to this is guy, where the GF’s are fully interacting and (up to self-consistent Born approximation) fully disorder averaged GF’s. But otherwise no impurity ladders, for simplicity.
And we get, supposedly:
Supposed to get same result at ω = 0 as for clean superconductor, a gap up till ω = 2Δ, and then non-zero behavior for ω > 2Δ. So altogether, identical to clean conductor, except for non-zero result for ω > 2Δ. And this must damp to zero eventually as ω continues to increase.

## Slide 45: Superconductors – Nonequilibrium Properties
Just throwing this out there as addendum. As one will suspect given prior results on the conductivity, the resistivity of our superconductor will precipitously drop to zero once the critical temperature has been reached. There doesn’t seem to be a major difference in behavior between Type I’s and Type II’s.