## Slide 1: Electron-Impurity Interaction
Like with metals, in the presence of impurities, the Hamiltonian for our valence electrons will be:
These impurities will replace the atoms in crystal lattice and therefore disrupt the periodicity of the potential, and thereby introduce the disorder potential referenced above. But these impurities will often be of group 13 (p-type: electron acceptor) or group 15 (n-type: electron donor). In this case, in addition to disrupting the periodic potential, they will provide additional states the valence electrons can jump into or out of. And they will also subtract electrons in the p-type case, or supply additional electrons in the n-type case. Take for instance Si. Then a p-type impurity would be Ga, and an n-type impurity would be As.

## Slide 2
Electron-Impurity Excitations
general picture of intrinsic semiconductor is this – see band gap.
we can dope with n-type impurity (say As), and electron levels look like below, with As’s last occupied level lying just below the Si lattice’s conduction band. At non-zero T, the donor electron can jump into conduction band.
and we can dope with p-type impurity (say Ga), and electron levels look like below, with Ga’s first unoccupied level lying just above the Si lattice’s valence band. At non-zero T, the electrons in the valence band can jump into the acceptor level.

## Slide 3
Electron-Impurity Excitations
Let’s think a little more closely about it. Consider n-type.
As has 5 valence electrons, compared to Ge’s 4. So when substitute As for Ge, there is one (donor) electron left over, and one unmatched As proton left over. If the unmatched proton weren’t there, the donor e would go into conduction band. But with the proton, it forms a hydrogenic bound state with a slightly lower energy (not full 13.6eV below because effective mass of conduction band is lower, and screening reduces strength of potential between proton and donor electron). So donor levels sit right below conduction band.
can represent situation schematically. Hydrogenic bound state has room for two electrons. Each donor level electron has energy εd above. But due to mutual repulsion, double occupation of donor level state is forbidden. So energies of the three situations displayed is:
E1 = 3εd
E2 = εd + ∞
E3 = εd + 2εc

## Slide 4
Electron-Impurity Excitations
Consider p-type.
Ga has 3 valence electrons, compared to Ge’s 4. So when substitute Ga for Ge, there is one missing electron needed to complete the covalent bond. Typically an electron will jump in to complete this bond, leaving a hole where it left, and increasing the charge of the Ga site by e. If the electron weren’t there, the (acceptor) hole would go into valence band. But with the electron, it forms a hydrogenic bound state with a slightly lower energy (not full 13.6eV because same reasons as before). And ‘lower’ for a hole is ‘higher’ for an electron. So the acceptor level sits a little above the valence band.
Can represent situation schematically. Each acceptor level electron has energy εa. Due to mutual repulsion, double hole occupation of acceptor level state is forbidden. Two electron occupation means one is captured to form the negative ‘nucleus’ and another to fill the ‘hole’, making it neutral. So no energy of interaction. The energy of the three situations displayed is:
E1 = 3εa
E2 = 3εa + ∞
E3 = 5εa - 2εv

## Slide 5
Electron-Impurity Thermal Equilibrium
T = 0
T > 0
thermal occupation of valence and conduction bands is as before.
conservation equation for particles/holes (N_d, N_a, N_v = density of respective levels).
occupation of donor/acceptor levels is:
now getting thermal occupations of valence, conductance bands, acceptor/donor levels.

## Slide 6
Electron-Impurity Thermal Equilibrium
so then plugging our results into the particle/hole conservation equation:
we can solve for the chemical potential, where μi and ni are the intrinsic chemical potential and carrier density, and ΔN = Nd – Na.
and with this, we can solve for the conduction/valence band particle/hole numbers. We find, in the limit of large ΔN,
to first order, this basically says Nd – Na electrons all reside in the conduction band, or Na – Nd holes all reside in the valence band, depending on which is larger, Nd or Na.

## Slide 7
Electron-Impurity Thermal Equilibrium
Here’s a picture of the equilibrium energy levels.
If Nd >> Na: In GS, Na electrons will drop out of donor level into acceptor level. At room temp, all remaining donor level electrons (ΔN = Nd – Na) will occupy conduction band, and ni2/ ΔN electrons from valence band will jump to conduction band too.
If Na >> Nd: In GS, Nd electrons will drop out of acceptor level into donor level. At room temp, all remaining acceptor level holes (ΔN = Na – Nd) will be occupied by electrons coming from the valence band, and ni2/ ΔN electrons from valence band will jump to conduction band too.

## Slide 8
Electron-Impurity Nonequilibrium
Let’s calculate the conductivity in the RTA approximation. We’ll look at the contribution from the conduction band first. General first order solution is:
for energies much greater than μ, we can make this approximation,
working out the derivative above, we find, to first order:
can form the current
in the DC limit,
and extract the conductivity

## Slide 9
Electron-Impurity Nonequilibrium
Now let’s look at the contribution from the valence band. The hole occupation, in the RTA approximation, is:
can form the current,
and extract the conductivity
and in the DC limit,

## Slide 10
Electron-Impurity Nonequilibrium
So altogether, we find:
If we’re doing intrinsic semiconductors, then nc = pv = ni, and we’ll find that σ increases with T. But if semiconductor is extrinsic, then nc = Nd – Na, or pv = Na – Nd, with little T dependence, and so it will more or less remain the same.
The mobility is a better indication of how ‘free’ the electrons are, since the conductivity includes fact that number of conducting electrons increases with T, not just how free they are. So mobility is proportionality between drift velocity and electric field,

## Slide 11: pn junction
For future reference, just good to have the following rough #’s mind, ostensibly for Si.
Also keep in mind the energy scales,

## Slide 12: pn junction
So now we’re looking at pn junction. The n-type semiconductor will have more electrons than the p-type, and so to even up the chemical potential, some will migrate to the p-type. This will create a net positive charge in the p-type, and net negative charge in the n-type, and will have the commensurate effect of creating an electric potential between across the junction. Since the electrons are negative, this will result in the electron energy levels in the p-type going up, and those in the n-type going down, an amount given by |e|φ. So those close to the junction will be hardly moved, while those far from the junction will be.
since the energy levels are altered, the electrons’ energy level thermal occupation numbers will also be altered. So we want to work out what the new populations are. To do this, we need to know what the potential is. We can do all this self-consistently.
I’m drawing the electron/hole distributions to first order, assuming ΔN >> ni, skipping the O(ni2/ΔN) contribution we talked about in the Thermal Equilibrium Properties file in the previous folder up.
depletion zone – so called because there are no (very few mobile carriers here)

## Slide 13: pn junction
First we’ll look at the charge density. So net charge density is (e negative),
And given a potential, the thermal occupation numbers are:
just observe that these formulas are roughly band degeneracy × classical thermal occupation number in grand canonical ensemble (with β negated for holes).
Close to the interface, this will work out to:
This equation basically says that all the electrons in the n-type drop out of the conduction and donor bands (an empty conduction and donor band would mean net charge (density) -eNd) and fill up the valence and acceptor bands (a full valence and acceptor band would mean a net charge (density) of eNa). Charge conservation will require Nadp = Nddn. The presence of completely filled or empty bands within the –dp < x < dn means there is no mobile charge here. So it is called the depletion zone.

## Slide 14: pn junction
Integrating twice, and employing the boundary conditions, we find:
And then we can fill this into Maxwell’s equation:
The ln term is negligible at room temperature, and so we see Δφ ~ Eg/|e| ~ O(V)
Filling numbers in here, we will find that these are on the order of nm’s.

## Slide 15: pn junction
Before we move on, let’s add back in a little detail. In the previous discussion, I said I neglected the presence of the ni2/ΔN electrons. We can add these back in to our thermal equilibrium picture – basically these electrons just jump up from the valence band into the conduction band.
a rough plot of the carrier densities.

## Slide 16: pn junction
And now let’s apply a potential difference, ΔV. We’ll assume it’s positively biased, and so goes counter the induced potential difference Δφ.
a rough plot of the carrier densities.
A few things change. ΔV drop occurs almost entirely across the depletion zone, as the depletion zone acts as an insulator. And in circuits, the applied potential difference is taken up almost entirely by the resistors as opposed to the wires. It also shrinks the spatial extent of the depletion zone. But it also stretches out the carrier density curve. So that a new zone opens up between the depletion zone and homogeneous zone – the diffusion zone.
In depletion zone, the electric field is strong, and carrier density gradient large – so get both drift and diffusion currents.
In diffusion zone, the electric field is weak, but carrier density gradient still relatively large, at least for majority carrier in that region – so get diffusion currents.
In homogeneous zone, the electric is small, but carrier densities larger. And carrier gradients are super small – so get just drift current.

## Slide 17: pn junction
Rough explanation of current.
The current can be thought of as being due to the movement of holes in the valence band and electrons in the conduction band. Consider holes in the valence band (similarly argument can be made for the electrons). We define:
jgen = current due to holes in n being pulled into p by the net E field. This is basically the drift current. Note this current is independent of the applied potential. Can argue that increasing ΔV decreases Δφeff and also decreases the depletion zone Δx. And so net field actually stays roughly same.
jrec = current due to holes in p being thermally activated up over the energy barrier Δφeff = Δφ – ΔV into n. This is basically the diffusion current.
Setting the sum of the two currents equal to zero when ΔV = 0 necessitates:
Note it increases w/o bound as ΔV >> 0 (since the potential barrier the hole has to surmount gets smaller and smaller), and drops to zero as ΔV << 0 (as the potential barrier the hole must surmount gets higher and higher).
And so our general expression for the net current is:

## Slide 18: pn junction
A less rough explanation of current. First we’ll look a elecrons.
Ssc describes scattering of electrons off of impurities. And Sgr (generation/recombination) describes electrons jumping into/out of the conduction band.
Now we’ll derive two balance equations. The first is the typical scattering one. We’ll multiply both sides by Nk, and integrate over k. The Sgr scattering term shouldn’t depend on k, I don’t think. So it would go to zero. Or better to say, it conserves momentum.
use relaxation time approximation on scattering term.
replace kikj with its average.
So we end up with:
the diffusion constant

## Slide 19: pn junction
Still looking at electrons. Now we’ll get the second equation. We’ll multiply both sides by N, and integrate over k. This time, the Ssc scattering term should vanish as it conserves particle number, but the Sgr term will not vanish, as it doesn’t conserve particle number.
use relaxation time approximation on scattering term.
So we end up with:
(IBP)  0

## Slide 20: pn junction
And now let’s do holes. Remembering for holes v = -k/m, rather than k/m, we have:
Ssc describes scattering of holes off of impurities. And Sgr (generation/recombination) describes electrons jumping into/out of the conduction band.
Now we’ll derive two balance equations. The first is the typical scattering one. We’ll multiply both sides by Nk, and integrate over k. The Sgr scattering term shouldn’t depend on k, I don’t think. So it would go to zero. Or better to say, it conserves momentum.
use relaxation time approximation on scattering term.
replace kikj with its average.
So we end up with:
the diffusion constant

## Slide 21: pn junction
Still looking at electrons. Now we’ll get the second equation. We’ll multiply both sides by N, and integrate over k. This time, the Ssc scattering term should vanish as it conserves particle number, but the Sgr term will not vanish, as it doesn’t conserve particle number.
use relaxation time approximation on scattering term.
So we end up with:
(IBP)  0

## Slide 22: pn junction
So our equations are, altogether,
where we now denote n by nc (conduction electron density), n(h) by pv (valence hole density), and nc(0), pv(0) are the equilibrium distributions. We’ll more or less take these equilibrium distributions to be:

## Slide 23: pn junction
Now we want to get the current. We can see from the prior equations that the current consists of a drift and diffusion part. But we can avoid having to evaluate both if we’re interested in the largest order contribution. So first consider the following simplification: since in the depletion zone E is large and nc, pv small, the speed of the charges must be large. And we’ll presume their transit time across the depletion zone is smaller than the generation-recombination time. That means we can eliminate the RHS of the right column of equations, and conclude that across the depletion zone jc,v are separately constant. So we can say,
We’re going to look at the steady state situation. So crossing out time-dependence, we have:

## Slide 24: pn junction
Again, dropping the drift current term as compared to the diffusion current, in our Boltzman equations, we can combine the electron equations together and the hole equations together to get these guys:
We can solve these equations
Our boundary conditions are given below:
So we almost have the carrier densities. We need to know nc(-dp) and pv(dn) in order to get the current. We can write down two more sets of equations for these guys.
These are the diffusion zone lengths.

## Slide 25: pn junction
One set comes from charge conservation. In the homogeneous zone, right up to the edge of the depletion zone, whatever charges are in the conduction band for x > dn come from Nd donor levels and pv holes in the valence band. And likewise whatever holes are in the valence band for x < -dp come from Na acceptor levels and whatever charges jumped into the conduction band.
Another set comes from the fact that inside the depletion zone, while the drift and diffusion currents are large, they nearly cancel (the difference being the net current of course). So it is approximately true that:
Filling in the diffusion constant, and relating the densities at –dp to those at dn, we can say,
And of course:

## Slide 26: pn junction
We can solve these two equations to find:
Now we’ll use a formula for the equilibrium potential difference:
and for the intrinsic carrier density:
to conclude,

## Slide 27: pn junction
Plugging these results back into the carrier density equations we have:
And then we can finally evaluate the current,
We get:
so when ΔV > 0 we get increasing current for increasing ΔV. I guess this is because larger ΔV means a smaller potential barrier for holes to travel from p to n. So jrec grows without bound as ΔV is increased, but jgen seems predominantly unaffected. But when the polarity of ΔV is reversed, this increases the size of the potential barrier, and so jrec shrinks to zero ultimately, while again, jgen is unaffected. So when ΔV < 0, we see the current saturates to a constant value.

## Slide 28: LEDs
And LED is basically a common pn junction. Current is applied in the usual forward direction.
So when we apply an electric field (battery) to our diode, the electric field will impart energy to the electrons/holes, and this energy is dissipated via scattering (quantified via τsc), but also by electrons dropping out of the conduction band and into the valence band (quantified via τgr). The former process will transform the energy acquired by the electric field into heat, while the latter will transform it into light, of frequency roughly equal to f = Eg/h, where Eg is the band gap energy. We can see that this latter process will only occur within the depletion + diffusion zone, since only there is (n – nc(0))/τgrc or (p – pv(0))/τgrv signficiant.
On a practical note, should mention that it can be difficult to see the light emitted from the diode. If Eg/h is not in the visible spectrum, then of course you won’t see it. But even if it is, a lot of the light that would get emitted from the depletion zone tends to get reflected back into the depletion zone, and reabsorbed eventually because the index of refraction of the homoegneous zone is higher than that of the depletion zone. Homogeneous zone has higher index of refraction, due to larger polarizability, say, or due to larger number of mobile electrons. So one has to make one end of the diode small so photons have better chance of transmitting through.

## Slide 29: Solar Cells
And a solar cell is basically an LED in reverse.
Thinking about the current in the jgen ~ jdrift vs. jrec ~ jdiff way, no net current will flow w/o light impinging on the N guy as, in equilibrium, the diffusion current of thermally excitated holes going over the potential barrier (from p to n) is canceled by the drift current of holes being dragged down the barrier by φ (from n to p). And similarly for electrons. But if we shine light on the N guy, then this can excite electrons from the valence band into the conduction band. When we bump an N electron into the conduction band, we are increasing pv, and visually it would seem, also decreasing ∇pv across the depletion zone. The increase in pv would increase |jdrift|, increasing current to left, while the decrease in ∇pv would decrease |jdiff|, also increasing the current to the left (remember e is negative, and ∇pv is negative). So this would seem to encourage flow of current from N to P. Apropos the electrons, we are increasing nc, and it seems, also increasing ∇nc across the depletion zone. The increase in nc would increase |jdrift|, increasing current to left, while the increase in ∇nc would increase |jdiff|, increasing the current to the right (remember e is negative). Well since three of the four currents got increased to the left, I’m going to go with the net current moving to the left. So,
Apropos the light, we’ll note that of course its frequency must be large enough to bump the electrons up from the valence band to the conduction band, so f = Eg/h, basically.

## Slide 30: MOSFETs
And last let’s look at a particular kind of transistor. We’ll discuss the MOSFET (Metal-Oxide-Semiconductor-Field-Effect-Transistor).
So it’s basically an npn junction, with a metal ‘gate’ attached via an SiO2 insulator/dielectric. The SiO2 is there to prevent leakage of mobile electrons from the gate into the p-type (the body). And the metal gate is there to apply a potential difference to the p-type (and n-types a little). When the applied potential difference to the metal gate is large (say φgate ~ Eg/|e|), then current can flow between source and drain (n→p→n); otherwise not.

## Slide 31: MOSFETs
Let’s turn off the potential difference between drain and source, and just consider the transistor by itself. When we first put the npn junction together, the N’s are at a higher chemical potential, as usual.
So electrons will migrate into the P, resulting in a depletion zone on either side of P. So in this configuration, no current can flow from N→P→N (beyond saturation current I guess).

## Slide 32: MOSFETs
Then when we apply an electric field in the z-direction (gate Voltage).
This lowers the energy levels in the p-type/body (and near the edges of the n-types). The amount of lowering would be proportional to the gate voltage potential. So it will be substantial at z = 0, and drop to zero as z increases. The new energy levels for some z close to z = 0, would look like this (the purple φ here below is the same φ as above and is not φeff = φ + φgate) :

## Slide 33: MOSFETs
I didn’t really show this in my picture, but typically the applied gate voltage would be large enough to pull the p-type conduction bands below the chemical potential (at least near the gate electrode). So φgae ~ Eg. And so of course electrons in the n-type conduction bands will drop into the p-type conduction bands. And electrons in the n-type valence bands will drop into the p-type valence bands (or could say holes in the p-type valence bands will ‘drop’ upwards into the n-type valence bands).
And so now the bands can conduct. And application of a potential difference between the source and drain will result in a current flow between them, and through the p-type. Note that since the energy band lowering won’t be too substantial for higher z’s, the region of conducting electrons will be limited to an effectively 2D region around the SiO2 insulator. So this is one way we can create and explore a 2D electron ‘gas’.